## Slide 1: Thermal Noise and Material Related Issues
Ronny Nawrodt1, Iain Martin2
23/08/2011
1Friedrich-Schiller-Universität Jena, Germany
2SUPA University of Glasgow, Scotland

## Slide 2: Overview
thermal noise in GW detectors (revision)
important material properties
mechanical loss measurements
  bulk
  coatings
(optics…)
summary

## Slide 3
Thermal noise in GW detectors

## Slide 4: Thermal noise in GW detectors
GW detectors are amongst the most sensitive tools today.
operation at the technical and scientifical limitations (noise, cross coupling, etc.)
improving the instruments means fighting with physics
  novel techniques (setups, cryogenics, etc.)
  novel materials (change of material for optical components)
  …

## Slide 5: Thermal noise in GW detectors
The first generation of interferometric GW detectors (LIGO, Virgo, GEO600, TAMA300) reached their design sensitivities in a wide range of frequencies.

## Slide 6: Thermal noise in GW detectors
current detectors are based on:
  fused silica optics (best optical material currently available)
  fused silica or metal suspensions
friction between the suspension and the optics can be avoided by using the low mechanical loss jointing technique of hydroxide catalysis bonding

## Slide 7: Thermal noise in GW detectors
Currently, the second generation of GW detectors is being built based on the experiences of the first generation of GW detectors and novel techniques that have been tested.
further improvements:
  aLIGO, aVirgo, GEO-HF fused silica, room temperatur,
  monolithic suspensions (demonstrated in GEO600 for years)
  LCGT + CLIO sapphire, cryogenics
pioneering work in the field of cryogenic large scale interferometry

## Slide 8: Thermal noise in GW detectors
As the second generation is designed and currently about to being built researchers started a conceptual design study for a 3rd generation detector – the Einstein Telescope design study.
aims:
  What technologies are needed to increase sensitivity by a factor of 10 compared to 2nd generation?
  How might such a design look like?
  Which materials should be used? Which design?
  (How much does it cost?)
homepage: www.et-gw.eu

## Slide 9: Thermal noise in GW detectors
artist view of ET – check www.et-gw.eu for details

## Slide 10: Thermal Noise in GW detectors
improvement of the sensitivity between different generations of GW detectors:

## Slide 11: Thermal noise in GW detectors
Parts of the Einstein Telescope have to be operated at cryogenic temperatures to reduce thermal noise.
natural links between ET and LCGT:
  cryogenics
  pulse tube vs. LHe cooling
  contamination of the mirrors due to cryotrapping
  general: pioneering technology in cryogenics
  people exchange between Japanese and Einstein Telescope researchers now extended through personal exchange program

## Slide 12: Thermal noise in GW detectors
a reminder of thermal noise:
  two different types
  (1) fluctuating thermal energy  Brownian thermal noise
  (2) fluctuating temperature  thermo-elastic, thermo-
  refractive, thermo-optic
  temperature dependent parameter (e.g. CTE, dn/dT) links temperature fluctuation and phase fluctuation of the detector

## Slide 13: Thermal noise in GW detectors
a reminder of bulk thermal noise
main message: material properties influence strongly the thermal noise – (nearly) all of them are temperature dependent
  Thermo-elastic noise:
  Brownian thermal noise:
beam diameter
temperature
=0 possible for some materials, e.g. silicon (@ 18 and 125 K)

## Slide 14: Thermal noise in GW detectors
a reminder of bulk thermal noise
similar with thermo-optical noise and finite corrections
Thermo-elastic noise:
Brownian thermal noise:
beam diameter
temperature

## Slide 15
Material properties

## Slide 16: Overview of material properties
mechanical properties
basic property: strength of the material (especially for suspension elements)
[IGR Glasgow]

## Slide 17: Overview of material properties
mechanical properties
Young‘s modulus, Poisson ratio
mass density of the material
available size
(growing methods)
optimum crystal orientation
mechanical loss to determine Brownian thermal noise
(= main focus of this lecture)
[Wacker]

## Slide 18: Overview of material properties
thermal properties
  strongly temperature dependent
  crystalline materials follow „basic“ thermodynamics / statistics
  (Debye theory)
  heat capacity (~ T3 at low temperatures for crystals)
  thermal conductivity (removal of heat!)
  coefficient of thermal expansion

## Slide 19: Overview of material properties
thermal properties
  thermal conductivity
increasing impurity
concentration (scattering
of phonons on impurities)
+ size effects (boundary scattering)
not enough phonons left
to carry heat
[Touloukian]
log scale 
log scale 

## Slide 20: Overview of material properties
thermal properties
  coeffcient of thermal expansion
  larger CTE for cryst. materials compare to amorphous (reason: summation of tiny effects in the crystal)
  usually CTE decreases with decreasing temperature
  some materials show temperatures with CTE = 0
  (e.g. silicon @ 18 and 125 K)

## Slide 21: Overview of material properties
optical properties
  refractive index n
  forming HR mirror coatings
  thermo-refractive coefficient dn/dT
  determines the thermo-refractive noise
  optical absorption 
  sets a fundamental limit to the minimum operational temperature

## Slide 22
Mechanical loss
- Introduction -

## Slide 23: Basics of mechanical loss
elastic behaviour of a solid
Hook‘s Law
… stress
… strain
E … Young‘s modulus
(German: modulus of elasticity)
instantaneous reaction, full recovery

## Slide 24: Basics of mechanical loss
anelastic behaviour of a solid
only partial instantaneous reaction, full recovery after t = 
anelasticity
relaxation

## Slide 25: Basics of mechanical loss
periodic process – anelasticity and mechanical loss
work
done on the
system
work
done by the
system
hysteresis
(= energy loss)

## Slide 26: Basics of mechanical loss
frequency f
energy dissipation per cycle
isothermal
adiabatic

## Slide 27: Basics of mechanical loss
definition of the mechanical loss = phase lag between stress and strain
measurement via the mechanical Q-factor at a resonance
keep in mind:
The mechanical loss is a continuous function of frequency but we just probe it at certain frequencies (resonant frequencies) of a system  no full knowledge available.

## Slide 28: Loss mechanisms
There are many different origins of loss in solids.
Focus on 3 dominant ones:
  phonon-phonon interaction
  thermo-elastic loss
  impurity driven losses
Phonon-phonon-damping (Akhiezer-/Landau-Rumer-Damping)
Phonons are forming a certain distribution when in equilibrium. At low frequency excitations the acoustic vibration (= phonon) modulates the lattice  new local
equilibrium  redistribution consumes energy  loss.

## Slide 29: Loss mechanisms
Phonon-phonon-damping (Akhiezer-/Landau-Rumer-Damping)
Phonons are forming a certain distribution when in equilibrium. At low frequency excitations the acoustic vibration (= phonon) modulates the lattice  new local
equilibrium  redistribution consumes energy  loss.
(Akhiezer loss)
If the phonon energy is high (high frequency vibration) the acoustic phonon directly interacts with the phonons of the given distribution  direct phonon scattering  redistribution consumes energy  loss.
(Landau-Rumer-Loss)

## Slide 30: Basics of mechanical loss
thermo-elastic damping
If a sample is deformed certain parts will be compressed or
expanded  local heating or cooling (depending on CTE).
Sample is now in thermal non-equilibrium  heat flux  entropy is increased  loss.
impurity driven damping
Impurities can occupy different positions in a lattice
depending on the applied stress. If an external vibration
is applied it might be energetic better to change positions  loss.

## Slide 31: Basics of mechanical loss
The transition between 2 (quasi-)stable positions can be modelled with a double-well potential:
 … relaxation strength
 … relaxation time
EA
energy
position
=0
0
„Debye peak“
EA … activation energy
0 … relaxation constant
thermally activated process:

## Slide 32: Basics of mechanical loss
ring-down measurements
bandwidth measurements
time
amplitude
f0
Df
frequency
amplitude

## Slide 33: Basics of mechanical loss
excitation of modes
  mechanical (e.g. piezo)
  electro-static
vibration read-out
  electrical read-out (capacitor)
  optical read-out (e.g. optical lever,
  interferometric techniques)
+
-
+

## Slide 34
Mechanical loss
- Bulk Materials -

## Slide 35: Selected examples - Quartz
crystalline quartz is well known  toy material to investigate setups and data processing tools
cryst. quartz shows channels along its c-axis
silicon
oxygen
hydrothermal growth of crystal
grown from solution under pressure
(~ 500 bar) at elevated temperatures
containing:
water
silicon dioxide
sodium carbonate / hydroxide

## Slide 36: Selected examples - Quartz
O
Si
impurities trapped in multiple well potential
along the c-axis
loss peaks associated with sodium
activation energy from experiment:
~ 55 meV
loss process is orientation dependent
detailed study needs different cryst.
cuts from the same material

## Slide 37: Selected examples – Fused Silica
fused silica:
very low loss at room temperature reaching 410-10
large loss peak around 30K
not suited for cryogenic
use in GW detectors
origin of the peak:
Amorphous silica has a near but no far order. Thus, loss processes get a distribution of loss parameters. The peak is the superposition of all of them.

## Slide 38: Selected examples – Sapphire/Silicon
crystalline materials needed for cryogenic operation
different candidate materials have been discussed in the past
possible candidate materials are sapphire (LCGT) and Si (ET)
reasons:
  both are optical materials (remember, FS is currently the best optical material)
  both are available in rather large pieces
  high thermal conductivity
  coating techniques available
while sapphire can be operated at 1064nm silicon demands a change of the laser wavelength due to its optical absorption

## Slide 39: Selected examples – Sapphire/Silicon
mechanical loss of silicon and sapphire is comparable at cryogenic temperatures (Q‘s up to several 109 achieved)
test measurement of silicon
and sapphire samples
[U Jena]

## Slide 40: Selected examples – Sapphire/Silicon
detailed investigation of intrinsic loss mechanisms in promising candidate bulk materials ongoing
questions:
  general loss processes?
  impurities? tolerable level of impurities?
  heat treatment to remove dislocations?
  surface loss?
  …
collaboration of several groups (Jena, Glasgow, Legnaro, starting collaboration with Japan) to investigate intrinsic damping of materials (coatings, bulk, surfaces, etc.)

## Slide 41
Mechanical loss
- Coating Materials -

## Slide 42: Optical coatings
Requirements – high reflectivity, low optical absorption (< 1ppm)
Multilayer coatings of dielectric materials, l/4 thick
Reflectivity from difference in refractive index, and number of layers, 2N.
Current detectors use silica (n=1.45) / tantala (n=2.03) coatings, ~ 15 bi-layers

## Slide 43: Coating thermal noise
Levin – interferometer most sensitive to mechanical loss close to the reflected laser beam
  Thus mechanical loss of coatings is particularly important
Coating loss dominated by the loss of the tantala layers
  ftantala ~ 410-4
  fsilica~ 510-5
Measurements suggested no observable loss from coating layer interfaces (however recent results from LMA, Lyon, suggest some interface loss may be observable)
Doping Ta2O5 with TiO2 can reduce the loss by ~40%.

## Slide 44: Coating thermal noise
Coating thermal noise expected to limit achievable sensitivity of future GW detectors at their most sensitive frequencies
Coating thermal noise

## Slide 45: Coating loss measurements
First cryogenic measurement of silica/tantala coating by Yamamoto et al, showed possible slight increase in loss at low temperature
Cryogenic loss studies of mono-layers of individual coating materials carried out in collaboration between Glasgow, Jena, LMA
  Study individual materials in isolation
  Identify microscopic dissipation mechanisms
  Test coating performance at cryogenic temperatures
Single layer coatings of silica (left) and tantala (right), clamped for loss measurements

## Slide 46: Measuring coating loss - 1
Single layers of a coating material applied to silicon cantilever substrates
Loss measured from exponential ring-down of bending modes
loss from free decay of amplitude
tantala coating
electrostatic
drive
34mm
500mm
50mm thick
Coating applied here
coated cantilever in clamp within cryostat
bending modes excited via eletrostatic drive

## Slide 47: Measuring coating loss - 2
Loss of coating layer calculated from difference in loss of a coated and un-coated cantilever
Scaling factor accounts for fraction of total elastic energy stored in the coating
Loss of (a) uncoated silicon cantilever with thermal oxide layer, (b) cantilever coated with 500 nm of TiO2-doped Ta2O5 (14.5% Ti) and (c) the calculated loss of the coating layer
(a)
(b)
(c)

## Slide 48: Loss peak analysis - tantala
Debye-like mechanical loss peaks
thermally activated process
 … relaxation strength
 … relaxation time
EA … activation energy
0 … relaxation constant
double well potential
without external stresses

## Slide 49: Loss mechanism parameters – Arrhenius plot
Activation energy
  (40 ± 3) meV for TiO2 doped Ta2O5
  (29 ± 2) meV for undoped Ta2O5
Doping with TiO2 increases the activation energy.
Transition between two stable states appears to be hindered

## Slide 50: Possible microscopic processes
no long-distance order in coating materials (amorphous)
possible transitions of atoms / atom groups
doping might block possible positions  increase of activation energy
Ta
Ta
O
O
Ta
Ta
O
Ti

## Slide 51: Distribution of model parameters
Debye loss peak plotted using calculated activation energy and relaxation constant
Much narrower than experimental peak
Amorphous structure results in a distribution of activation energies.

## Slide 52: Distribution of parameters
refined model:
asymmetric double-well
potential
barrier height distribution g(V)
asymmetry distribution f(D)
g represents the coupling between strain and the dissipation mechanism
Cii is the elastic constant of the material
[Gilroy, Phillips 1981]

## Slide 53: Distribution of barrier heights
asymmetric double well potential:
barrier height distribution
contains information about
the microscopic structure
doping changes height and
distribution of barrier heights
g(V) … barrier height distribution
[Gilroy, Phillips 1981]
[Martin et al. 2009]
g(V)f0

## Slide 54: Effect of heat treatment temperature on Ta2O5 loss
Three loss peaks, triggered at different post-deposition heat-treatment temperatures
(i)
300C
600 C
800 C
400C
800 C
800 C
600 C
800 C
600 C
800 C
600 C
800 C
400C
600 C
800 C
400C
600 C
800 C
300C
400C
600 C
800 C
Loss at 1.9 kHz of 0.5 mm thick un-doped Ta2O5 coatings heat treated at 300, 400, 600 and 800 C. (Coatings from CSIRO)

## Slide 55: Effect of heat treatment temperature on Ta2O5 loss
35 K peak
  Observed in Ta2O5 heat treated at 300, 400 C, and likely in Ta2O5 heat treated at 600 C
  Activation energy 54 meV
  Analogous to dissipation peak in fused silica, involving thermally activated transitions of oxygen atoms?
300C
600 C
800 C
400C
(i)
300 C
800 C
800 C
600 C
800 C
600 C
800 C
600 C
800 C
400C
600 C
800 C
400C
600 C
800 C
300C
400C
600 C
800 C
300C
400C
600 C
800 C
Above: Electron diffraction pattern of Ta2O5 heat treated at 600 C
Left: Loss at 1.9 kHz of 0.5 mm Ta2O5 coatings annealed at 300, 400, 600 and 800 C.

## Slide 56: Effect of heat treatment temperature on Ta2O5 loss
18 K peak
  Observed in Ta2O5 heat treated at 600 C and 800 C
  Related to structural changes brought on by heat treatment close to crystallisation temperature?
Above: Electron diffraction pattern of Ta2O5 heat treated at 600 C
Left: Loss at 1.9 kHz of 0.5 mm Ta2O5 coatings annealed at 300, 400, 600 and 800 C.
300C
600 C
800 C
400C
(i)
600 C
800 C
800 C
600 C
800 C
600 C
800 C
600 C
800 C
400C
600 C
800 C
400C
600 C
800 C
300C
400C
600 C
800 C
300C
400C
600 C
800 C

## Slide 57: Effect of heat treatment temperature on Ta2O5 loss
90 K peak
  Observed in coating heat treated at 800 C
  Large, broad loss peak likely to be related to (expected) onset of polycrystalline structure due to high temperature heat treatment. Loss mechanism could be e.g. phonon scattering at grain boundaries
Above: Electron diffraction pattern of Ta2O5 heat treated at 800 C
Left: Loss at 1.9 kHz of 0.5 mm Ta2O5 coatings annealed at 300, 400, 600 and 800 C.
300C
600 C
800 C
400C
(i)
800 C
800 C
600 C
800 C
600 C
800 C
600 C
800 C
400C
600 C
800 C
400C
600 C
800 C
300C
400C
600 C
800 C
300C
400C
600 C
800 C
800 C
800 C

## Slide 58: Loss of silica coatings
Scatter at higher temperatures, possibly due to loss into clamp.
Loss of SiO2 will have a significant contribution to coating thermal noise below 100 K
Repeated room temperature measurement of silica coating loss.

## Slide 59: Coating thermal noise at 100 Hz
If coating loss was constant with temperature, could gain factor of ~ 4 in TN at 18 K
Measured coating losses imply we can only gain a factor of ~ 1.7 in coating TN by cooling to 18 K
Optimistic estimate – coating loss remains constant at all T
Using measured coating loss
Optimistic estimate – coating loss remains constant at all T
Using measured coating loss

## Slide 60: Probing links between atomic structure and loss
Short range structure of amorphous materials probed by Reduced Density Function analysis of TEM electron diffraction data
  RDF is a Fourier transform of the information gained from the intensity profile of a diffraction pattern
  RDF gives statistical representation of where atoms are located with respect to a central atom

## Slide 61: The Reduced Density Function (RDF)
Interpreting RDFs
  Peak position - nearest neighbour distances
  Peak height – nearest neighbour abundances
  Peak width – indicates level of order in structure
RDFs of heat-treated tantala coatings1
r (Å)
G(r)
G(r)
G(r)
G(r)
Ta O distance
Ta Ta distance

## Slide 62: Structural modelling
RDF can be used as basis for Reverse Monte Carlo models of the microstructure, allowing e.g. bond angle distributions to be extracted
  Molecular dynamics simulations used to ensure models are energetically stable
Bond angle (degrees)
Distribution
Ta – blue O - red

## Slide 63: Current / future coatings research
Alternative high-index coating materials e.g. amorphous Si, hafnia
Alternative low-index materials e.g. Al2O3
Exploring links between short-range atomic structure and loss
Reduced coating / coating-free optics – diffractive optics and resonant waveguide mirrors

## Slide 64
Optical Properties

## Slide 65: Important Properties
refractive index n  influences coating selection
thermo-refractive coefficient dn/dT  governs the thermo-refractive noise
optical absorption   limits the operation at low temperatures and at high laser powers
all these parameters are needed at low temperatures!

## Slide 66: Research on the refractive index of Si at low temperatures
classical prism experiment needed to determine refractive index
method of minimum deviation with high resolution cryogenic actuators
method of minimum deviation
in Littrow-order
experimental setup for cryogenic
measurements of the refractive index
A – laser, B – beam splitter, C – Faraday isolator, D – cryostat, E- prism, F- detector

## Slide 67: Research on the thermo-refractive coefficient of Si
incoming light
outcoming light
internal reflections
Fabry-Perot-Cavity
filled with silicon, dn/dT
determines optical path
length inside FPC

## Slide 68: Research on the optical absorption of silicon at low T.
simplified electronic band structure
direct transition
indirect transition
phonon contribution
k
Dk = 0
photons do not
carry momentum
Dk = kphonon
Ephoton + Ephonon = E
photons with E < Egap=1.1eV can be
absorbed by assistance of phonons
VB
CB

## Slide 69: Research on the optical absorption of silicon at low T.
300 K
1 phonon
2 phonons
3 phonons
[Keeves et al., J. Appl. Phys.]
photon
phonon
density of phonons is strongly temperature dependent
much smaller absorption can be expected at low temperatures
 measurements ongoing

## Slide 70
Summary

## Slide 71: What have we learned?
material properties strongly determine the thermal noise performance of a detector
simple temperature scaling is dangerous and leads to wrong results
impurities determine mechanical losses  strong influence on thermal noise
material science (understanding temperature behaviour of parameters) is needed to optimise future detectors
a wide and open field…